## Slide 1
1.
INTRODUCTION TO
POLYMER BLENDING

## Slide 2
Size of initial
polymer pellets
( 1 to 5 mm)
Flow, melting, mixing, reaction, structuring
Size of final
polymer particles
( 0.1 to 5 µm;
10 to 100 nm)
Twin screw extruder
A continuous process
Short residence times ( < 60 s)
Throughput of a few tons per hour

## Slide 3
Twin screw extruders

## Slide 4
The geometry of kneading discs and flow channel
Flow channel
KD1: 45/5/32
KD2: 60/4/32
KD3: 90/5/32
KD5: 90/5/64
KD4: 90/10/64

## Slide 5
MORPHOLOGY
Block
copolymer
Graft
copolymer
Morphology = f(Mixing, Compatibilizer)

## Slide 6
A BATCH MIXER

## Slide 7
Emulsification curve
Construction of an emulsificaiton curve
is tedious and material-consuming,
especially for industrial processes.
Blend:
1000 kg/h
Compatibilizer:
>10 kg/h
PS/PA6

## Slide 8
2.
CONCEPT OF
COMPATIBILIZER-TRACER

## Slide 9
Concept of compatibilizer-tracer
Fluorescent moities
Zhang, Cai-Liang; Feng, Lian-Fang; Hoppe, Sandrine;
Hu, Guo-Hua. AIChE Journal (2009), 55, 279-283.
Zhang, Cai-Liang; Feng, Lian-Fang; Hoppe, Sandrine;
Hu, Guo-Hua. AIChE Journal (2012), 58,1931-1928.

## Slide 10
Schematic of a fluorescent
bifurcated optical probe

## Slide 11
(a) Non-reactive blending processes

## Slide 12
PS+PA6
Screw extruder
PS-g-PA-tracer
RTD and dispersed domain
size distribution (DSD)
RTD
DSD

## Slide 13
DSD
RTD

## Slide 14
An emulsification curve
from RTD & DSD
Unique feature:
two curves that
form a closed loop.
Short time domain
Long time domain

## Slide 15
Concept of compatibilizer-tracer
Construction of emulsification curves
for industrial polymer blending processes
Molecular design of the compatibilizer
Mixing assessement
Process design
Process optimization

## Slide 16
Comparison between two mixers

## Slide 17
Effect of screw speed on
the emulsification curve

## Slide 18
(b) Reactive blending processes

## Slide 19
Reactive compatibilizer-tracer
PS-co-TMI-Ant
N
C
O
N
C
O
PS
PA6-NH2
Interfacial Reaction
PS-g-PA6 graft copolymers
PS/PA6
PS-co-TMI-Ant

## Slide 20
A
B
1 to 5 nm

## Slide 21
RTD
DSD

## Slide 22: Two PS-TMI-Ant with 1% and 8% TMI

## Slide 23: Two reactive compatibilizers with different reactive groups
Anh-PS-Ant
N
C
O
N
C
O
PS-co-TMI-Ant
Notes: This slice compared the efficiency of block or graft copolymer as tracer. The molecular structures of two reactive tracer-emulsifier show in left figure. Emulsification curve corresponding to the long time domain is above the one corresponding to short time domain for Anh-PS-Ant as tracer-emulsifier; while emulsification curves for PS-co-TMI-Ant as tracer-emulsifier are almost superposition. This indicated that the reaction of PS-co-TMI-Ant with polyamide 6 is faster than that of Anh-PS-Ant.

## Slide 24
4.
CONCLUSIONS
AND
FUTURE WORK

## Slide 25
Concept of compatibilizer-tracer
(reactive or not)
Construction of emulsification curves
for industrial polymer blending processes
Molecular design of the compatibilizer
Assessement of mixing mechanisms
mixing efficiency
Modeling & model validation
Design of screw profile & proces
Process optimization

## Slide 26
Flow-induced copolymer pull-out
Inoue et al.